## Slide 1
nextnano GmbH, Garching b. München, Germany
www.nextnano.com
stefan.birner@nextnano.com
How to treat Quaternaries in nextnano
2017-Dec-15
Dr. Stefan Birner, Managing Director

## Slide 2: Material parameters needed
GaAs/AlGaAs heterostructures (no strain)
effective masses (me, mhh, mlh, mso, ...) or k∙p parameters
band gap Egap, split-off energy
band offsets (CBO, VBO)
dielectric constant (Poisson equation)

## Slide 3: Ternaries
Linear interpolation
Quadratic interpolation using a constant bowing parameter
Interpolation using a bowing parameter which depends on alloy content x

## Slide 4: Ternaries
Ternary
Binaries GaAs, AlAs  Ternary AlxGa1-xAs = x AlAs + (1-x) GaAs
Bowing parameter C
– C x (1-x)
– C(x) x (1-x)
might depend on alloy content x

## Slide 5: Quaternaries
Quaternary: AlxGa1-xAsyP1-y III-III-V-V
III-III-III-V, III-V-V-V

## Slide 6: Quaternaries
AlxGa1-xIn1-x-yAs
III-III-III-V
III-V-V-V
10 parameters!

## Slide 7: Quaternaries
AlxGa1-xAsyP1-y III-III-V-V
13 parameters!

## Slide 8: Material parameters needed
GaAs/InGaAs heterostructures (strain!)
... +
lattice constant
elastic constants (2-3 parameters)
piezoelectric constant
deformation potentials (3-8 parameters)

## Slide 9: nextnano++ software
http://www.nextnano.com/nextnanoplus/software_documentation/database/zincblende.htm
http://www.nextnano.com/nextnanoplus/software_documentation/input_file/structure.htm

## Slide 10: More information
PhD thesis T. Zibold (Appendix E)
http://www.nextnano.com/information/publications.php
nextnano³ software http://www.nextnano.com/nextnano3/input_parser/database/docu/quaternaries.htm http://www.nextnano.com/nextnano3/tutorial/1Dtutorial_AlGaInP_onGaAs.htm